Table S1

Composition data

| Glass Family | Chalcogenide Glass Composition | Measured Density (gm/cc) | Calc. Density (gm/cc) | Ref. |
| --- | --- | --- | --- | --- |
| Ge-Ga-Se | 80 GeSe2 - 20 Ga2Se3 | 4.420 | 4.370 | DA33 |
| Ge-Ga-S | 75 GeS2-25 Ga2S3 | 2.955 | 2.867 | DA12 |
| Ge-Ga-S | 83 GeS2-17 Ga2S3 | 2.891 | 2.830 | DA12 |
| Se | Se | 4.276 | 4.275 | DA29 |
| Ge-Ga-Se | Ge16-Ga20-Se64 | 4.450 | 4.450 | DA29 |
| Ge-Ga-Se | Ge19-Ga5-Se76 | 4.340 | 4.313 | DA29 |
| Ge-Ga-Se | Ge16-Ga5-Se79 | 4.360 | 4.308 | DA29 |
| Ge-Ga-Se | Ge15-Ga10-Se75 | 4.420 | 4.339 | DA29 |
| Ge-As-Se | Ge5.56-As33.33-Se61.1 | 4.579 | 4.589 | DA33 |
| Ge-As-Se-Pb | Ge5.35-As32.09-Se60.7-Pb1.86 | 4.688 | 4.710 | DA33 |
| Ge-As-Se-Pb | Ge5-As30-Se60-Pb5 | 4.850 | 4.938 | DA33 |
| Ge-As-Se-Pb | Ge4-As26.1-Se58.5-Pb11.4 | 5.221 | 5.480 | DA33 |
| Ge-Te | Ge-Te4 | 5.499 | 5.506 | DA01 |
| Ge-Te | Ge-Te5 | 5.540 | 5.539 | DA01 |
| Ge-Sb-S-Te | Ge10-Sb30-S50-Te10 | 4.290 | 4.425 | DA02 |
| Ge-Sb-S-Te | Ge20-Sb20-S50-Te10 | 3.950 | 4.016 | DA02 |
| Ge-Sb-S-Te | Ge20-Sb20-S54.7-Te5.3 | 3.760 | 3.820 | DA02 |
| Ge-Sb-S-Te | Ge25.4-Sb13.3-S51.1-Te10.2 | 3.740 | 3.745 | DA02 |
| Ge-Sb-S-Te | Ge25.2-Sb13.1-S56.4-Te5.3 | 3.540 | 3.521 | DA02 |
| As-Se | As33.33-Se66.67 | 4.560 | 4.583 | DA03 |
| As-Se-Cu | As32.79-Se65.57-Cu1.64 | 4.632 | 4.627 | DA03 |
| As-Se-Cu | As32.23-Se64.52-Cu3.22 | 4.671 | 4.670 | DA03 |
| As-Se-Cu | As30.3-Se60.6-Cu9.1 | 4.880 | 4.840 | DA03 |
| As-Se-Cu | As28.57-Se57.14-Cu14.29 | 5.072 | 5.003 | DA03 |
| As-Se-Cu | As25-Se50-Cu25 | 5.440 | 5.384 | DA03 |
| Ge-As-Se | Ge5-As5-Se90 | 4.349 | 4.307 | DA04 |
| Ge-As-Se | Ge5-As20-Se75 | 4.472 | 4.439 | DA04 |
| Ge-As-Se | Ge10-As20-Se70 | 4.486 | 4.446 | DA04 |
| Ge-As-Se | Ge10-As10-Se80 | 4.405 | 4.351 | DA04 |
| Ge-As-Se | Ge15-As10-Se75 | 4.421 | 4.359 | DA04 |
| Ge-As-Se | Ge20-As5-Se75 | 4.397 | 4.331 | DA04 |
| Ge-As-Se | Ge15-As20-Se65 | 4.474 | 4.455 | DA04 |
| Ge-Se | Ge15-As0-Se85 | 4.357 | 4.295 | DA04 |
| Ge-Se | Ge10-As0-Se90 | 4.341 | 4.287 | DA04 |
| Ge-Se | Ge20As0-Se80 | 4.362 | 4.304 | DA04 |
| As-Se | As15-Se85 | 4.390 | 4.383 | DA05 |
| As-Se | As20-Se80 | 4.430 | 4.433 | DA05 |
| As-Se | As25-Se75 | 4.490 | 4.487 | DA05 |
| As-Te-Se | As30-Se50-Te20-Ga00 | 4.888 | 4.886 | DA06 |
| Ga-As-Te-Se | As29-Se50-Te20-Ga1 | 4.912 | 4.875 | DA06 |
| Ge-Sb-Se | Ge26.67-Sb8-Se65.33 | 4.580 | 4.520 | DA07 |
| Ge-Sb-Se | Ge23.33-Sb12-Se64.67 | 4.730 | 4.651 | DA07 |
| Ge-Sb-Se | Ge20-Sb16-Se64 | 4.880 | 4.797 | DA07 |
| Ge-Sb-Se | Ge31.67-Sb2-Se66.33 | 4.350 | 4.365 | DA07 |
| Ge-Sb-Se | Ge30-Sb4-Se66 | 4.440 | 4.410 | DA07 |
| Ge-Sb-Se | Ge13.33-Sb24-Se62.67 | 5.180 | 5.119 | DA07 |
| Ge-Sb-Se | Ge16.67-Sb20-Se63.33 | 5.040 | 4.954 | DA07 |
| As-Si-Te | Si10-As20-Te70 | 5.270 | 5.331 | DA08 |
| As-Si-Te | Si10-As25-Te65 | 5.260 | 5.321 | DA08 |
| As-Si-Te | Si10-As40-Te50 | 5.090 | 5.292 | DA08 |
| As-Si-Te | Si15-As40-Te45 | 4.880 | 5.116 | DA08 |
| As-Si-Te | Si20-As10-Te70 | 4.960 | 5.052 | DA08 |
| As-Si-Te | Si20-As15-Te65 | 4.900 | 5.028 | DA08 |
| Ge-As-Se | AMTIR-1 | 4.415 | 4.408 | DA09 |
| As-Se | AMTIR-2 | 4.597 | 4.632 | DA09 |
| As-Se | AMTIR-4 | 4.498 | 4.528 | DA09 |
| As-Se | AMTIR-5 | 4.606 | 4.620 | DA09 |
| As-S | AMTIR-6 | 3.187 | 3.192 | DA09 |
| As-Se | AMTIR-7 | 4.538 | 4.575 | DA09 |
| Ge-Sb-Se | Ge28-Sb12-Se60 | 4.656 | 4.660 | DA10 |
| As-Se | As40-Se60 | 4.633 | 4.661 | DA10 |
| As-S | As40-S60 | 3.202 | 3.192 | DA10 |
| Ge-As-Se-Bi | Ge2.97-As19.49-Se60.59-Bi16.95 | 5.623 | 5.609 | DA13 |
| Ge-As-Se-Bi | Ge4.35-As26.09-Se60.87-Bi8.70 | 5.184 | 5.157 | DA13 |
| Ge-As-Se-Bi | Ge5.07-As30.40-Se61.01-Bi3.52 | 4.881 | 4.831 | DA13 |
| Ge-Se | Ge17-Se83 | 4.340 | 4.298 | DA14 |
| Ge-Ga-Se | Ge16-Se79-Ga5 | 4.360 | 4.308 | DA14 |
| Ge-Ga-Se | Ge15-Se75-Ga10 | 4.420 | 4.339 | DA14 |
| Ge-Ga-Se | Ge14-Se71-Ga15 | 4.500 | 4.386 | DA14 |
| Ge-Se | Ge20-Se80 | 4.230 | 4.304 | DA14 |
| Ge-Ga-Se | Ge19-Se76-Ga5 | 4.340 | 4.313 | DA14 |
| Ge-Ga-Se | Ge18-Se72-Ga10 | 4.380 | 4.344 | DA14 |
| Ge-Ga-Se | Ge17-Se68-Ga15 | 4.440 | 4.392 | DA14 |
| Ge-Ga-Se | Ge16-Se64-Ga20 | 4.450 | 4.450 | DA14 |
| Ge-Te-Ag-I | 97.5(GeTe4.3) - 2.5(AgI) | 5.559 | 5.534 | DA15 |
| Ge-Te-Ag-I | 95(GeTe4.3) - 5(AgI) | 5.591 | 5.551 | DA15 |
| Ge-Te-Ag-I | 93(GeTe4.3) - 7(AgI) | 5.648 | 5.565 | DA15 |
| Ge-Te-Ag-I | 90(GeTe4.3) - 10(AgI) | 5.758 | 5.588 | DA15 |
| Ge-Te-Ag-I | 85(GeTe4.3) - 15(AgI) | 5.867 | 5.631 | DA15 |
| Ge-Te-Ag-I | 80(GeTe4.3) - 20(AgI) | 5.951 | 5.679 | DA15 |
| Ge-Te-Ag-I | 83(GeTe4.3) - 17(AgI) | 5.900 | 5.682 | DA15 |
| Ge-Te-Ag-I | 82(GeTe4.3) - 18(AgI) | 5.880 | 5.659 | DA15 |
| Ge-Zn-Se | (GeSe3)90 - (ZnSe)10 - (Ag2Se)0 | 4.360 | 4.199 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)81 - (ZnSe)9 - (Ag2Se)10 | 4.550 | 4.489 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)72 - (ZnSe)8 - (Ag2Se)20 | 4.680 | 4.791 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)63 - (ZnSe)7 - (Ag2Se)30 | 5.020 | 5.110 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)54 - (ZnSe)6 - (Ag2Se)40 | 5.582 | 5.450 | DA16 |
| Ge-Zn-Se | (GeSe3)80 - (ZnSe)20 - (Ag2Se)0 | 4.450 | 4.340 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)72 - (ZnSe)18 - (Ag2Se)10 | 4.690 | 4.627 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)56 - (ZnSe)14 - (Ag2Se)30 | 5.280 | 5.232 | DA16 |
| As-Sb-Se | As35-Sb15-Se50 | 4.990 | 5.091 | DA17 |
| As-Sb-Se | As30-Sb15-Se55 | 4.983 | 5.026 | DA17 |
| As-Sb-Se | As25-Sb15-Se60 | 4.980 | 4.962 | DA17 |
| As-Sb-Se | As20-Sb15-Se65 | 4.920 | 4.901 | DA17 |
| As-Sb-Se | As10-Sb15-Se75 | 4.850 | 4.793 | DA17 |
| As-Sb-Se | As35-Sb5-Se60 | 4.730 | 4.722 | DA17 |
| As-Sb-Se | As30-Sb10-Se60 | 4.860 | 4.828 | DA17 |
| As-Sb-Se | As22-Sb18-Se60 | 5.040 | 5.051 | DA17 |
| Te-Se | (Te)8 - (Sn)0 - (Se)92 | 4.376 | 4.415 | DA18 |
| Te-Sn-Se | (Te)7 - (Sn)1 - (Se)92 | 4.301 | 4.407 | DA18 |
| Te-Sn-Se | (Te)6 - (Sn)2 - (Se)92 | 4.309 | 4.403 | DA18 |
| Te-Sn-Se | (Te)5 - (Sn)3 - (Se)92 | 4.314 | 4.402 | DA18 |
| Te-Sn-Se | (Te)4 - (Sn)4 - (Se)92 | 4.318 | 4.404 | DA18 |
| Te-Sn-Se | (Te)3 - (Sn)5 - (Se)92 | 4.325 | 4.409 | DA18 |
| Ge-Se | (Ge)10 - (Se)90 - (Te)0 | 4.362 | 4.287 | DA19 |
| Ge-Te-Se | (Ge)10 - (Se)80 - (Te)10 | 4.533 | 4.462 | DA19 |
| Ge-Te-Se | (Ge)10 - (Se)70 - (Te)20 | 4.687 | 4.625 | DA19 |
| Ge-Te-Se | (Ge)10 - (Se)60 - (Te)30 | 4.863 | 4.777 | DA19 |
| Ge-Te-Se | (Ge)10 - (Se)50 - (Te)40 | 5.028 | 4.921 | DA19 |
| Ge-Te-Se | (Ge)10 - (Se)40 - (Te)50 | 5.179 | 5.057 | DA19 |
| As-S | (As)2 - (S)3 | 3.170 | 3.192 | DA21 |
| As-Se-S | (As)40 - (S)45- (Se)15 | 3.530 | 3.513 | DA21 |
| As-Se-S | (As)40 - (S)30- (Se)30 | 3.860 | 3.838 | DA21 |
| As-Se-S | (As)40 - (S)15- (Se)45 | 4.200 | 4.150 | DA21 |
| As-Se-S | (As)32 - (S)34 - (Se)34 | 3.700 | 3.687 | DA21 |
| As-Se-S | (As)24 - (S)38 - (Se)38 | 3.610 | 3.538 | DA21 |
| As-S | (As)24 - (S)76 | 2.670 | 2.667 | DA21 |
| As-Se-S | (As)24 - (S)57 - (Se)19 | 3.129 | 3.105 | DA21 |
| As-Se-S | (As)24 - (S)19 - (Se)57 | 4.050 | 3.915 | DA21 |
| As-Se | (As)24 - (Se)76 | 4.460 | 4.476 | DA21 |
| As-Se-S | (As)18 - (S)41 - (Se)41 | 3.510 | 3.430 | DA21 |
| Ge-Se | Ge20-Se80 | 4.345 | 4.304 | DA22 |
| Ge-In-Se | Ge-19-Se76-In5 | 4.552 | 4.402 | DA22 |
| Ge-In-Se | Ge-18-Se72-In10 | 4.673 | 4.493 | DA22 |
| Ge-In-Se | Ge-17-Se68-In15 | 4.715 | 4.579 | DA22 |
| Ge-In-Se | Ge-16-Se64-In20 | 4.780 | 4.661 | DA22 |
| Ge-Se | Ge-16.67-Se83.34-In0 | 4.235 | 4.298 | DA22 |
| Ge-In-Se | Ge-15.83-Se79.17-In5 | 4.421 | 4.396 | DA22 |
| Ge-In-Se | Ge-15-Se75-In10 | 4.637 | 4.488 | DA22 |
| Ge-In-Se | Ge-14.17-Se70.83-In15 | 4.652 | 4.574 | DA22 |
| Ge-In-Se | Ge-13.33-Se66.67-In20 | 4.615 | 4.656 | DA22 |
| Ge-Ga-Sb-S | (Ga)5-(Ge)25-(Sb)5-(S)65 | 3.100 | 2.941 | DA24 |
| Ge-Ga-Sb-S | (Ga)1-(Ge)29-(Sb)5-(S)65 | 3.000 | 2.941 | DA24 |
| Ge-Ga-Sb-S | (Ga)1-(Ge)24-(Sb)5-(S)70 | 2.890 | 2.819 | DA24 |
| Ge-Ga-Sb-S | (Ga)5-(Ge)20-(Sb)10-(S)65 | 3.210 | 3.096 | DA24 |
| Ge-Ga-Sb-S | (Ga)10-(Ge)15-(Sb)10-(S)65 | 3.260 | 3.113 | DA24 |
| Ge-Ga-Sb-S | (Ga)5-(Ge)20-(Sb)5-(S)70 | 2.940 | 2.819 | DA24 |
| Ge-Sb-Se | (GeSe2)94-(Sb)6 | 4.630 | 4.467 | DA25 |
| Ge-Sb-Se | (GeSe2)88-(Sb)12 | 4.850 | 4.663 | DA25 |
| Ge-Sb-Se | (GeSe3.5)90-(Sb)10 | 4.770 | 4.573 | DA25 |
| Ge-Sb-Se | (Ge28Sb12Se60) | 4.670 | 4.660 | DA25 |
| Ge-Sn-S | (Ge0.8Sn0.2S3) | 2.750 | 2.674 | DA25 |
| Ge-Sn-S | (Ge0.7Sn0.3S3) | 2.860 | 2.742 | DA25 |
| Ge-Sn-S | (Ge0.6Sn0.4S3) | 2.940 | 2.818 | DA25 |
| Ge-Bi-S | (Ge20Bi5S75) | 3.010 | 2.970 | DA25 |
| Ge-Bi-S | (Ge20Bi10S70) | 3.430 | 3.471 | DA25 |
| Ge-Bi-S | (Ge20Bi15S65) | 3.840 | 3.943 | DA25 |
| Ge-Se | (GeSe2) | 4.450 | 4.328 | DA25 |
| Ge-Sn-Se | (Ge0.9Sn0.1Se2) | 4.390 | 4.369 | DA25 |
| Ge-S | (Ge20S80) | 2.560 | 2.447 | DA25 |
| Ge-S | (GeS2) | 2.760 | 2.776 | DA25 |
| Ge-Ga-S | (GeS2)90-(Ga)10 | 2.900 | 2.942 | DA25 |
| Ge-Te | (GeTe4) | 5.499 | 5.506 | DA01 |
| Ge-Te-Ag | (GeTe4)95-(Ag)5 | 5.730 | 5.690 | DA01 |
| Ge-Te-Ag | (GeTe4)90-(Ag)10 | 5.858 | 5.880 | DA01 |
| Ge-Te-I | (GeTe4)95-(I)5 | 5.408 | 5.516 | DA01 |
| Ge-Te-Ag-I | (GeTe4)95-(AgI)5 | 5.587 | 5.596 | DA01 |
| Ge-Te-Ag-I | (GeTe4)90-(AgI)10 | 5.662 | 5.699 | DA01 |
| Ge-Te-Ag-I | (GeTe4)87.5-(AgI)12.5 | 5.680 | 5.755 | DA01 |
| Ge-Te-Ag-I | (GeTe4)85-(AgI)15 | 5.719 | 5.814 | DA01 |
| Ge-Te-Ag-I | (GeTe4)82.5-(AgI)17.5 | 5.728 | 5.875 | DA01 |
| Ge-Te-Ag-I | (GeTe4)80-(AgI)20 | 5.760 | 5.940 | DA01 |
| Ge-As-Se | Ge11-As22-Se67 | 4.488 | 4.469 | DA26 |
| Ge-As-Se | Ge17.5-As11-Se71.5 | 4.424 | 4.372 | DA26 |
| Ge-As-Se | Ge11.5-As24-Se64.5 | 4.495 | 4.492 | DA26 |
| Ge-As-Se | Ge18-As23-Se59 | 4.434 | 4.492 | DA26 |
| Ge-As-Se | Ge22-As24-Se54 | 4.449 | 4.510 | DA26 |
| Ge-As-Se | Ge35-As15-Se50 | 4.441 | 4.439 | DA26 |
| Ge-As-Se | Ge39-As16-Se45 | 4.571 | 4.455 | DA26 |
| Ge-As-Se | Ge7.5-As15-Se77.5 | 4.429 | 4.392 | DA26 |
| Ge-As-Se | Ge12.5-As5-Se82.5 | 4.384 | 4.318 | DA26 |
| Ge-As-Se | Ge5-As30-Se65 | 4.538 | 4.550 | DA26 |
| Ge-As-Se | Ge7.5-As35-Se57.5 | 4.450 | 4.612 | DA26 |
| Ge-As-Se | Ge10-As30-Se60 | 4.469 | 4.557 | DA26 |
| Ge-As-Se | Ge12.5-As25-Se62.5 | 4.493 | 4.505 | DA26 |
| Ge-As-Se | Ge15-As20-Se65 | 4.450 | 4.505 | DA26 |
| Ge-As-Se | Ge20-As10-Se70 | 4.412 | 4.368 | DA26 |
| Ge-As-Se | Ge22.5-As5-Se72.5 | 4.384 | 4.336 | DA26 |
| Ge-As-Se | Ge10-As35-Se55 | 4.471 | 4.615 | DA26 |
| Ge-As-Se | Ge15-As25-Se60 | 4.448 | 4.509 | DA26 |
| Ge-As-Se | Ge22.5-As10-Se67.5 | 4.394 | 4.373 | DA26 |
| Ge-As-Se | Ge20-As20-Se60 | 4.441 | 4.464 | DA26 |
| Ge-As-Se | Ge25-As10-Se65 | 4.363 | 4.377 | DA26 |
| Ge-As-Se | Ge30-As10-Se60 | 4.348 | 4.386 | DA26 |
| Ge-As-Se | Ge25-As20-Se55 | 4.425 | 4.473 | DA26 |
| Ge-As-Se | Ge21-As30-Se49 | 4.472 | 4.576 | DA26 |
| Ge-As-Se | Ge27-As18-Se55 | 4.424 | 4.455 | DA26 |
| Ge-As-Se | Ge30-As20-Se50 | 4.478 | 4.481 | DA26 |
| Ge-As-Se | Ge35-As10-Se55 | 4.400 | 4.395 | DA26 |
| Ge-As-Se | Ge5-As10-Se85 | 4.390 | 4.344 | DA26 |
| Ge-As-Se | Ge7.5-As10-Se82.5 | 4.391 | 4.347 | DA26 |
| Ge-As-Se | Ge12.5-As10-Se77.5 | 4.410 | 4.355 | DA26 |
| Ge-As-Se | Ge17.5-As10-Se72.5 | 4.422 | 4.364 | DA26 |
| Ge-As-Se | Ge27.5-As10-Se62.5 | 4.345 | 4.382 | DA26 |
| Ge-As-Se | Ge22-As20-Se58 | 4.430 | 4.467 | DA26 |
| Ge-As-Se | Ge33-As20-Se47 | 4.491 | 4.486 | DA26 |
| Ge-Te | Ge20-Te80 | 5.499 | 5.506 | DA22 |
| Ge-In-Te | Ge17-Te68-In15 | 5.370 | 5.586 | DA22 |
| Ge-Te | Ge17-Te83 | 5.540 | 5.536 | DA22 |
| Ge-In-Te | Ge16-Te79-In5 | 5.430 | 5.568 | DA22 |
| Ge-In-Te | Ge14-Te71-In15 | 5.540 | 5.615 | DA22 |
| Ge-In-Te | Ge13-Te67-In20 | 5.550 | 5.633 | DA22 |
| As-Se-Te | As0.4 Se0.35 Te0.25 | 4.990 | 5.078 | DA30 |
| As-Se-Te-Cu | As0.4 Se0.35 Te0.25 Cu.05 | 5.180 | 5.196 | DA30 |
| As-Se-Te-Cu | As0.4 Se0.35 Te0.25 Cu.075 | 5.250 | 5.254 | DA30 |
| As-Se-Te-Cu | As0.4 Se0.35 Te0.25 Cu.1 | 5.300 | 5.311 | DA30 |
| As-Se-Te-Cu | As0.4 Se0.35 Te0.25 Cu.125 | 5.350 | 5.367 | DA30 |
| As-Se-Te-Cu | As0.4 Se0.35 Te0.25 Cu.15 | 5.400 | 5.422 | DA30 |
| Ge-Sb-S | Ge40-Sb5-S55 | 3.260 | 3.182 | DA31 |
| Ge-Sb-S | Ge35-Sb10-S55 | 3.410 | 3.338 | DA31 |
| Ge-Sb-S | Ge35-Sb5-S60 | 3.150 | 3.063 | DA31 |
| Ge-Sb-S | Ge30-Sb15-S55 | 3.550 | 3.515 | DA31 |
| Ge-Sb-S | Ge30-Sb10-S60 | 3.270 | 3.218 | DA31 |
| Ge-Sb-S | Ge25-Sb20-S55 | 3.690 | 3.707 | DA31 |
| Ge-Sb-S | Ge25-Sb15-S60 | 3.410 | 3.395 | DA31 |
| Ge-Sb-S | Ge25-Sb10-S65 | 3.120 | 3.097 | DA31 |
| Ge-Sb-S | Ge25-Sb7.5-S67.5 | 3.000 | 2.956 | DA31 |
| Ge-Sb-S | Ge23-Sb12-S65 | 3.188 | 3.165 | DA31 |
| Ge-Sb-S | Ge20-Sb25-S55 | 3.850 | 3.911 | DA31 |
| Ge-Sb-S | Ge20-Sb20-S60 | 3.540 | 3.586 | DA31 |
| Ge-Sb-S | Ge15-Sb25-S60 | 3.690 | 3.789 | DA31 |
| Ge-Sb-S | Ge15-Sb20-S65 | 3.430 | 3.464 | DA31 |
| Si-As-Te | Si37-As30-Te33 | 4.240 | 4.341 | DA32 |
| Si-As-Te | Si35-As25-Te40 | 4.330 | 4.453 | DA32 |
| Si-As-Te-Se-Ag | Si35-As23-Te35-Se5-Ag2 | 4.340 | 4.415 | DA32 |
| Si-As-Te-Se-Ag | Si35-As23-Te30-Se10-Ag2 | 4.260 | 4.313 | DA32 |
| Si-As-Te-Se-Ag | Si35-As23-Te20-Se20-Ag2 | 4.100 | 4.125 | DA32 |
| Si-As-Te-Ag | Si35-As20-Te40-Ag5 | 4.500 | 4.639 | DA32 |
| Si-As-Te-Se-Ag | Si35-As20-Te18-Se22-Ag5 | 4.150 | 4.200 | DA32 |
| Si-As-Te-Se-Ag | Si35-As17-Te15-Se25-Ag8 | 4.250 | 4.258 | DA32 |
| Si-As-Te-Se-Ag | Si35-As15-Te18-Se22-Ag10 | 4.360 | 4.389 | DA32 |
| Si-As-Te-Se-Ag | Si35-As15-Te10-Se30-Ag10 | 4.270 | 4.241 | DA32 |
| As-Se-Te | 1(As0.40Se0.35Te0.25) | 4.990 | 5.078 | DA30 |
| As-Se-Te-Cu | 0.95(As0.40Se0.35Te0.25) + 0.05 Cu | 5.180 | 5.203 | DA30 |
| As-Se-Te-Cu | 0.925(As0.40Se0.35Te0.25) + 0.075 Cu | 5.250 | 5.268 | DA30 |
| As-Se-Te-Cu | 0.9(As0.40Se0.35Te0.25) + 0.1 Cu | 5.300 | 5.336 | DA30 |
| As-Se-Te-Cu | 0.875(As0.40Se0.35Te0.25) + 0.125 Cu | 5.350 | 5.406 | DA30 |
| As-Se-Te-Cu | 0.85(As0.40Se0.35Te0.25) + 0.15 Cu | 5.400 | 5.480 | DA30 |
| Ge Se | Ge/Se Ratio 0/100 | 4.280 | 4.275 | DA34 |
| Ge Se | Ge/Se Ratio 5/95 | 4.310 | 4.280 | DA34 |
| Ge Se | Ge/Se Ratio 10/90 | 4.340 | 4.287 | DA34 |
| Ge Se | Ge/Se Ratio 15/85 | 4.360 | 4.295 | DA34 |
| Ge Se | Ge/Se Ratio 20/80 | 4.370 | 4.304 | DA34 |
| Ge Se | Ge/Se Ratio 25/75 | 4.360 | 4.313 | DA34 |
| Ge Se | Ge/Se Ratio 30/70 | 4.320 | 4.322 | DA34 |
| Ge Se | Ge/Se Ratio 40/60 | 4.360 | 4.340 | DA34 |
| Ge Sb Se | (Ge28Sb12Se60) | 4.740 | 4.660 | DA35 |
| Ge Sb Se Ag | (Ge28Sb12Se60)0.95 + (Ag)0.05 | 5.000 | 4.887 | DA35 |
| Ge Sb Se Ag | (Ge28Sb12Se60)0.9 + (Ag)0.1 | 5.250 | 5.122 | DA35 |
| Ge Sb Se Ag | (Ge28Sb12Se60)0.85 + (Ag)0.15 | 5.500 | 5.365 | DA35 |
| Ge Sb Se Ag | (Ge28Sb12Se60)0.8 + (Ag)0.2 | 5.800 | 5.619 | DA35 |
| Ge As Se Pb | (Ge33As12Se55)0.99 + (Pb)0.01 | 4.540 | 4.476 | DA35 |
| Ge As Se Pb | (Ge33As12Se55)0.97 + (Pb)0.03 | 4.700 | 4.622 | DA35 |
| Ge As Se Pb | (Ge33As12Se55)0.95+ (Pb)0.05 | 4.850 | 4.779 | DA35 |
| Ge As Se Pb | (Ge33As12Se55)0.93 + (Pb)0.07 | 5.100 | 4.947 | DA35 |
| Ge As Se Pb | (Ge33As12Se55)0.91 + (Pb)0.09 | 5.300 | 5.124 | DA35 |
| Si-As-Te-Se-Ag | Si35-As23-Te25-Se15-Ag2 | 4.170 | 4.217 | DA32 |
| Si-As-Te-Se-Ag | Si35-As20-Te35-Se5-Ag5 | 4.450 | 4.526 | DA32 |
| Si-As-Te-Se-Ag | Si35-As20-Te30-Se10-Ag5 | 4.280 | 4.424 | DA32 |
| Si-As-Te-Se-Ag | Si35-As20-Te20-Se20-Ag5 | 4.220 | 4.236 | DA32 |
| Si-As-Te-Ag | Si35-As17-Te40-Ag8 | 4.710 | 4.753 | DA32 |
| Si-As-Te-Se-Ag | Si35-As17-Te35-Se5-Ag8 | 4.580 | 4.639 | DA32 |
| Si-As-Te-Se-Ag | Si35-As17-Te30-Se10-Ag8 | 4.470 | 4.537 | DA32 |
| Si-As-Te-Se-Ag | Si35-As17-Te28-Se12-Ag8 | 4.430 | 4.498 | DA32 |
| Si-As-Te-Se-Ag | Si35-As17-Te20-Se20-Ag8 | 4.280 | 4.349 | DA32 |
| Si-As-Te-Se-Ag | Si35-As15-Te35-Se5-Ag10 | 4.720 | 4.716 | DA32 |
| Si-As-Te-Se-Ag | Si35-As15-Te30-Se10-Ag10 | 4.610 | 4.613 | DA32 |
| Si-As-Te-Se-Ag | Si35-As15-Te25-Se15-Ag10 | 4.490 | 4.517 | DA32 |
| Si-As-Te-Se-Ag | Si35-As15-Te20-Se20-Ag10 | 4.390 | 4.426 | DA32 |
| Ge-Se-Sb-Te | (GeSe2)90 (Sb2Te3)10 | 4.498 | 4.516 | DA37 |
| Ge-Se-Sb-Te-Pb | (GeSe2)90 (PbSb2Te4)10 | 4.530 | 4.579 | DA37 |
| Ge-Se-Sb-Te-Pb | (GeSe2)85.5 (Sb2Te3)4.5 (PbSb2Te4)10 | 4.648 | 4.665 | DA37 |
| Ge-Se-Sb-Te-Pb | (GeSe2)81 (Sb2Te3)9 (PbSb2Te4)10 | 4.745 | 4.757 | DA37 |
| Ge-Se-Sb-Te-Pb | (GeSe2)72 (Sb2Te3)18 (PbSb2Te4)10 | 5.046 | 4.948 | DA37 |
| Ge-Se-Sb-Te-Pb | (GeSe2)72 (Sb2Te3)8 (PbSb2Te4)20 | 4.925 | 5.007 | DA37 |
| Ge-Bi-Se-Cd | (GeSe2)81(Bi2Se3)9(CdSe)10 | 4.840 | 4.837 | DA16 |
| Ge-Bi-Se-Cd | (GeSe2)85.5(Bi2Se3)4.5(CdSe)10 | 4.750 | 4.703 | DA16 |
| Ge-Bi-Se-Cd | (GeSe2)80.75(Bi2Se3)14.25(CdSe)5 | 4.900 | 4.866 | DA16 |
| Se-Zn | Se98Zn2 | 3.980 | 4.123 | DA16 |
| Se-S-Zn | Se87S10Zn3 | 3.700 | 3.806 | DA16 |
| Se-S-Zn | Se77S20Zn3 | 3.500 | 3.605 | DA16 |
| Se-S-Zn | Se73S25Zn2 | 3.480 | 3.510 | DA16 |
| Se-S-Zn | Se71S25Zn4 | 3.420 | 3.528 | DA16 |
| Se-S-Zn | Se67S30Zn3 | 3.380 | 3.425 | DA16 |
| Ge-Se-Zn | Ge2Se96Zn2 | 3.990 | 4.125 | DA16 |
| Ge-Se-Zn | Ge10Se88Zn2 | 4.020 | 4.133 | DA16 |
| Ge-Se-Zn | Ge20Se78Zn2 | 4.040 | 4.147 | DA16 |
| Ge-Se-Zn | Ge29Se69Zn2 | 4.070 | 4.161 | DA16 |
| Ge-Se-Zn | Ge39Se59Zn2 | 4.120 | 4.176 | DA16 |
| Ge-Sb-Se-Cd | (GeSe2)72 (Sb2Se3)18(CdSe)10 | 4.600 | 4.737 | DA16 |
| Ge-Sb-Se-Cd | (GeSe2)42(Sb2Se3)28(CdSe)30 | 5.130 | 5.266 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)81 (ZnSe)9 (Ag2Se)10 | 4.550 | 4.489 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)72 (ZnSe)8 (Ag2Se)20 | 4.680 | 4.789 | DA16 |
| Ge-Zn-Se-Ag | (GeSe3)56 (ZnSe)14 (Ag2Se)30 | 5.280 | 5.232 | DA16 |
| Ge-Sb-Se | (Ge)28 - (Sb)12 - (Se)60 | 4.680 | 4.660 | DA20 |
| As-Se | (As)40 - (Se)60 | 4.630 | 4.661 | DA20 |
| Ge-As-Se | Ge33-As12-Se55 | 4.410 | 4.408 | DA38 |
| Ge-As-Se-Te | Ge30-As32-Se13-Te25 | 4.840 | 5.036 | DA38 |
| Ge-As-Se | Ge10-As40-Se50 | 4.470 | 4.674 | DA38 |
| Ge-As-Se | Ge22-As20-Se58 | 4.440 | 4.467 | DA38 |
| As-Si-Te | As15-Si10-Te75 | 5.363 | 5.343 | DA08 |
| As-Si-Te | As30-Si10-Te60 | 5.258 | 5.311 | DA08 |
| As-Si-Te | As35-Si10-Te55 | 5.279 | 5.302 | DA08 |
| As-Si-Te | As45-Si10-Te45 | 5.105 | 5.280 | DA08 |
| As-Si-Te | As50-Si10-Te40 | 5.125 | 5.268 | DA08 |
| As-Si-Te | As10-Si15-Te75 | 5.299 | 5.207 | DA08 |
| As-Si-Te | As15-Si15-Te70 | 5.176 | 5.187 | DA08 |
| As-Si-Te | As20-Si15-Te65 | 5.135 | 5.171 | DA08 |
| As-Si-Te | As27-Si14-Te59 | 5.207 | 5.185 | DA08 |
| As-Si-Te | As30-Si15-Te55 | 5.094 | 5.144 | DA08 |
| As-Si-Te | As35-Si15-Te50 | 5.094 | 5.131 | DA08 |
| As-Si-Te | As45-Si15-Te40 | 4.920 | 5.100 | DA08 |
| As-Si-Te | As50-Si15-Te35 | 4.941 | 5.082 | DA08 |
| As-Si-Te | As5-Si20-Te75 | 5.115 | 5.082 | DA08 |
| As-Si-Te | As25-Si20-Te55 | 4.889 | 4.990 | DA08 |
| As-Si-Te | As30-Si20-Te50 | 4.889 | 4.973 | DA08 |
| As-Si-Te | As45-Si20-Te35 | 4.848 | 4.774 | DA08 |
| As-Si-Te | As24-Si26-Te50 | 4.715 | 4.787 | DA08 |
| As-Si-Te | As30-Si25-Te45 | 4.746 | 4.795 | DA08 |
| As-Si-Te | As35-Si25-Te40 | 4.766 | 4.772 | DA08 |
| As-Si-Te | As40-Si25-Te35 | 4.654 | 4.747 | DA08 |
| As-Si-Te | As45-Si25-Te30 | 4.628 | 4.721 | DA08 |
| As-Si-Te | As20-Si30-Te50 | 4.628 | 4.666 | DA08 |
| As-Si-Te | As40-Si30-Te30 | 4.590 | 4.583 | DA08 |
| As-Si-Te | As40-Si35-Te25 | 4.325 | 4.349 | DA08 |
| As-Si-Te | As50-Si13-Te37 | 5.061 | 5.157 | DA08 |
| Se | Se 100 | 4.270 | 4.275 | DA36 |
| S-Se | S10-Se90 | 4.063 | 3.939 | DA36 |
| S-Se | S30-Se70 | 3.612 | 3.550 | DA36 |
| S-Se | S45-Se55 | 3.275 | 3.254 | DA36 |
| S-Se | S60-Se40 | 2.916 | 2.921 | DA36 |
| S-Se 4.283 | S75-Se25 | 2.548 | 2.560 | DA36 |
| Se-I | Se99.5 -I0.5 | 4.277 | 4.282 | DA36 |
| Se-I | Se99.0 -I1.0 | 4.277 | 4.289 | DA36 |
| Se-I | Se98.5 -I1.5 | 4.283 | 4.297 | DA36 |
| Se-I | Se98.0 -I2.0 | 4.283 | 4.305 | DA36 |
| Se-I | Se97.0 -I3.0 | 4.287 | 4.322 | DA36 |
| Ge-Ga-Se-Pb | 90(GeSe2)-5(Ga2Se3)-5(PbSe) | 4.430 | 4.439 | DA40 |
| Ge-Ga-Se-Pb | 80(GeSe2)-10(Ga2Se3)-10(PbSe) | 4.560 | 4.564 | DA40 |
| Ge-Ga-Se | 80(GeSe2)-20(Ga2Se3) | 4.390 | 4.370 | DA40 |
| Ge-Ga-Se-Pb | 75(GeSe2)-5(Ga2Se3)-20(PbSe) | 4.950 | 4.848 | DA40 |
| Ge-Ga-Se-Pb | 75(GeSe2)-18.75(Ga2Se3)-6.25(PbSe) | 4.630 | 4.497 | DA40 |
| Ge-Ga-Se-Pb | 70(GeSe2)-10(Ga2Se3)-20(PbSe) | 4.960 | 4.841 | DA40 |
| Ge-Ga-Se-Pb | 70(GeSe2)-20(Ga2Se3)-10(PbSe) | 4.570 | 4.588 | DA40 |
| Ge-Ga-Se-Pb | 66.67(GeSe2)-16.67(Ga2Se3)-16.67(PbSe) | 4.930 | 4.751 | DA40 |
| Ge-Ga-Se-Pb | 60(GeSe2)-15(Ga2Se3)-25(PbSe) | 5.310 | 4.995 | DA40 |
| Ge-Ga-Se-Pb | 60(GeSe2)-30(Ga2Se3)-10(PbSe) | 4.640 | 4.625 | DA40 |
| Ge-Ga-Se | 90(GeSe2)-10(Ga2Se3) | 4.200 | 4.336 | DA40 |
| Ge-Ga-Se | 85(GeSe2)-15(Ga2Se3) | 4.360 | 4.351 | DA40 |
| Ge-Ga-Se | 80(GeSe2)-20(Ga2Se3) | 4.390 | 4.370 | DA40 |
| Ge-Ga-Se | 75(GeSe2)-25(Ga2Se3) | 4.390 | 4.392 | DA40 |
| Ge-In-Se | 90(GeSe2)-0(Ga2Se3)-10(In2Se3) | 4.390 | 4.443 | DA40 |
| Ge-In-Se | 85(GeSe2)-0(Ga2Se3)-15(In2Se3) | 4.430 | 4.492 | DA40 |
| Ge-In-Se | 80(GeSe2)-0(Ga2Se3)-20(In2Se3) | 4.580 | 4.535 | DA40 |
| Ge-In-Se | 70(GeSe2)-0(Ga2Se3)-30(In2Se3) | 4.710 | 4.612 | DA40 |
| Ge-Ga-In-Se | 80(GeSe2)-5(Ga2Se3)-15(In2Se3) | 4.550 | 4.486 | DA40 |
| Ge-Ga-In-Se | 80(GeSe2)-10(Ga2Se3)-10(In2Se3) | 4.490 | 4.443 | DA40 |
| Ge-Ga-In-Se | 80(GeSe2)-15(Ga2Se3)-5(In2Se3) | 4.430 | 4.405 | DA40 |
| Ge-Ga-In-Se | 75(GeSe2)-5(Ga2Se3)-20(In2Se3) | 4.640 | 4.529 | DA40 |
| Ge-Ga-In-Se | 75(GeSe2)-6.25(Ga2Se3)-18.75(In2Se3) | 4.560 | 4.518 | DA40 |
| Ge-Ga-In-Se | 75(GeSe2)-18.75(Ga2Se3)-6.25(In2Se3) | 4.490 | 4.430 | DA40 |
| Ge-Ga-In-Se | 70(GeSe2)-20(Ga2Se3)-10(In2Se3) | 4.520 | 4.469 | DA40 |
| Ge-Ga-In-Se | 70(GeSe2)-25(Ga2Se3)-5(In2Se3) | 4.450 | 4.442 | DA40 |
| Ge-Ga-In-Se | 65(GeSe2)-10(Ga2Se3)-25(In2Se3) | 4.700 | 4.569 | DA40 |
| Ge-Ga-In-Se | 65(GeSe2)-25(Ga2Se3)-10(In2Se3) | 4.530 | 4.487 | DA40 |
| Ge-Ga-In-Se | 60(GeSe2)-10(Ga2Se3)-30(In2Se3) | 4.720 | 4.604 | DA40 |
| Ge-Ga-In-Se | 60(GeSe2)-15(Ga2Se3)-25(In2Se3) | 4.650 | 4.575 | DA40 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.1-As0.1-Te0.8 ) 95 | 5.567 | 5.472 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.1-As0.2-Te0.7 ) 95 | 5.496 | 5.447 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.1-As0.3-Te0.6 ) 95 | 5.428 | 5.434 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.1-As0.4-Te0.5 ) 95 | 5.342 | 5.422 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.1-As0.5-Te0.4 ) 95 | 5.304 | 5.407 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.1-As0.6-Te0.3 ) 95 | 5.268 | 5.387 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.2-As0.1-Te0.7 ) 95 | 5.428 | 5.372 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.2-As0.2-Te0.6 ) 95 | 5.333 | 5.343 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.2-As0.3-Te0.5 ) 95 | 5.238 | 5.325 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.2-As0.4-Te0.4 ) 95 | 5.201 | 5.307 | DA39 |
| Se-(Ge-As-Te) | Se 5 - ( Ge0.2-As0.5-Te0.3 ) 95 | 5.144 | 5.286 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.1-As0.1-Te0.8 ) 90 | 5.485 | 5.400 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.1-As0.2-Te0.7 ) 90 | 5.367 | 5.373 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.1-As0.3-Te0.6 ) 90 | 5.323 | 5.357 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.1-As0.4-Te0.5 ) 90 | 5.224 | 5.342 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.1-As0.5-Te0.4 ) 90 | 5.136 | 5.324 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.1-As0.6-Te0.3 ) 90 | 5.110 | 5.303 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.2-As0.1-Te0.7 ) 90 | 5.334 | 5.303 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.2-As0.2-Te0.6) 90 | 5.223 | 5.272 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.2-As0.3-Te0.5) 90 | 5.199 | 5.251 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.2-As0.4-Te0.4) 90 | 5.122 | 5.231 | DA39 |
| Se-(Ge-As-Te) | Se 10 - ( Ge0.2-As0.5-Te0.3) 90 | 5.079 | 5.208 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.1-As0.1-Te0.8) 86 | 5.413 | 5.349 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.1-As0.2-Te0.7) 86 | 5.359 | 5.320 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.1-As0.3-Te0.6) 86 | 5.259 | 5.302 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.1-As0.4-Te0.5) 86 | 5.203 | 5.285 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.1-As0.5-Te0.4) 86 | 5.104 | 5.267 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.1-As0.6-Te0.3) 86 | 5.058 | 5.244 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.2-As0.1-Te0.7) 86 | 5.280 | 5.255 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.2-As0.2-Te0.6) 86 | 5.199 | 5.222 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.2-As0.3-Te0.5) 86 | 5.138 | 5.199 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.2-As0.4-Te0.4) 86 | 5.026 | 5.178 | DA39 |
| Se-(Ge-As-Te) | Se 14 - ( Ge0.2-As0.5-Te0.3) 86 | 4.999 | 5.154 | DA39 |
| Ge-As-S | Ge6-As36-S58 | 3.150 | 3.209 | DA41 |
| As-Sb-S | As36-Sb6-S58 | 3.410 | 3.373 | DA41 |
| Ge-Sb-S | Ge23-Sb7-S70 | 2.930 | 2.880 | DA41 |
| Ge-Ga-Se-Cs-Cl | 70GeSe2 - 20Ga2Se3 - 10CsCl | 4.274 | 4.279 | DA42 |
| Ge-Ga-S-Se-Cs-Cl | 70GeSe2 - 20Ga2S3 - 10CsCl | 3.907 | 3.747 | DA42 |
| Ge-Ga-Se | 70GeSe2 - 30Ga2Se3 | 4.400 | 4.415 | DA42 |
| Ge-Ga-S-Se | 70GeSe2 - 30Ga2S3 | 3.900 | 3.725 | DA42 |
| Ge-Ga-Se | 77.778GeSe2 - 22.222Ga2Se3 | 4.380 | 4.379 | DA42 |
| Ge-Ga-S-Se | 77.778GeSe2 - 22.222Ga2S3 | 3.930 | 3.809 | DA42 |
| Ge-Ga-S | 80GeS2 - 20Ga2S3 | 2.789 | 2.843 | DA43 |
| Ge-Ga-S-Cs-Cl | (80GeS2 - 20Ga2S3)95 - (CsCl)5 | 2.951 | 2.872 | DA43 |
| Ge-Ga-S-Cs-Cl | (80GeS2 - 20Ga2S3)90 - (CsCl)10 | 2.959 | 2.896 | DA43 |
| Ge-Ga-S-Cs-Cl | (80GeS2 - 20Ga2S3)85 - (CsCl)15 | 2.977 | 2.914 | DA43 |
| Ge-Ga-S-Cs-Cl | (80GeS2 - 20Ga2S3)80 - (CsCl)20 | 2.972 | 2.927 | DA43 |
| Ge-Ga-S | 25(Ga2S3)-75(GeS2) | 2.784 | 2.867 | DA44 |
| Ge-Ga-S-Cs-Cl | 25(Ga2S3)-65(GeS2)-10(CsCl) | 2.960 | 2.910 | DA44 |
| Ge-Ga-S-Cs-Cl | 25(Ga2S3)-62.5(GeS2)-12.5(CsCl) | 2.990 | 2.920 | DA44 |
| Ge-Ga-S-Cs-Cl | 25(Ga2S3)-50(GeS2)-25(CsCl) | 3.050 | 2.961 | DA44 |
| Ge-Ga-S-Cs-Cl | 25(Ga2S3)-37.5(GeS2)-37.5(CsCl) | 3.103 | 2.992 | DA44 |
| Ge-Ga-S-Cs-Cl | 25(Ga2S3)-30(GeS2)-45(CsCl) | 3.135 | 3.004 | DA44 |
| Ge-Ga-S-Cs-Cl | 25(Ga2S3)-25(GeS2)-50(CsCl) | 3.175 | 3.010 | DA44 |
| Ge-Ga-S-Cs-Cl | 30(Ga2S3)-50(GeS2)-20(CsCl) | 3.021 | 2.969 | DA44 |
| Ge-Ga-S-Cs-Cl | 35(Ga2S3)-35(GeS2)-30(CsCl) | 3.105 | 3.021 | DA44 |
| Ge-Ga-S-Cs-Cl | 35(Ga2S3)-25(GeS2)-40(CsCl) | 3.124 | 3.043 | DA44 |
| Ge-Ga-S-Cs-Cl | 37.5(Ga2S3)-20(GeS2)-42.5(CsCl) | 3.144 | 3.059 | DA44 |
| Ge-Ga-S-Cs-Cl | 15(Ga2S3)-45(GeS2)-40(CsCl) | 3.045 | 2.951 | DA44 |
| Ge-Sb-S | (GeS2-Sb2S3)100 (CsCl)0 | 3.660 | 3.727 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)95 (CsCl)5 | 3.560 | 3.681 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)90 (CsCl)10 | 3.560 | 3.633 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)85 (CsCl)15 | 3.520 | 3.582 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)80 (CsCl)20 | 3.520 | 3.531 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)75 (CsCl)25 | 3.370 | 3.479 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)70 (CsCl)30 | 3.350 | 3.427 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)65 (CsCl)35 | 3.260 | 3.376 | DA45 |
| Ge-Sb-S-Cs-Cl | (GeS2-Sb2S3)60 (CsCl)40 | 3.230 | 3.326 | DA45 |
| Ge-Ga-S | [GeS2]0.80[Ga2S3]0.20 | 2.800 | 2.813 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).95 (CsCl).05 | 2.910 | 2.845 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).925 (CsCl).075 | 2.930 | 2.859 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).90 (CsCl).10 | 2.920 | 2.871 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).875 (CsCl).125 | 2.960 | 2.882 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).85 (CsCl).15 | 2.960 | 2.892 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).825 (CsCl).175 | 2.970 | 2.900 | DA46 |
| Ge-Ga-S-Cs-Cl | ([GeS2]0.80[Ga2S3]0.20).8 (CsCl).2 | 3.040 | 2.908 | DA46 |
| Ge-Ga-S-Cd-I | ([GeS2]0.80[Ga2S3]0.20).95 (CdI2).05 | 3.000 | 3.034 | DA46 |
| Ge-Ga-S-Cd-I | ([GeS2]0.80[Ga2S3]0.20).925 (CdI2).075 | 3.090 | 3.148 | DA46 |
| Ge-Ga-S-Cd-I | ([GeS2]0.80[Ga2S3]0.20).9 (CdI2).1 | 3.190 | 3.264 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).95 (CsI).05 | 2.950 | 2.900 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).925 (CsI).075 | 3.020 | 2.941 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).9 (CsI).1 | 3.070 | 2.981 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).875 (CsI).125 | 3.090 | 3.019 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).85 (CsI).15 | 3.100 | 3.056 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).825 (CsI).175 | 3.130 | 3.091 | DA46 |
| Ge-Ga-S-Cs-I | ([GeS2]0.80[Ga2S3]0.20).8 (CsI).2 | 3.160 | 3.125 | DA46 |
| Ge-Ga-S-Cd-Cl | ([GeS2]0.80[Ga2S3]0.20).95 (CdCl2).05 | 2.860 | 2.959 | DA46 |
| Ge-Ga-S-Cd-Cl | ([GeS2]0.80[Ga2S3]0.20).925 (CdCl2).075 | 2.940 | 3.035 | DA46 |
| As-S | As40S60 | 3.200 | 3.192 | DA47 |
| As-S-Se | As40S45Se15 | 3.560 | 3.513 | DA47 |
| As-S-Se | As40S30Se30 | 3.920 | 3.838 | DA47 |
| As-S-Se | As40S15Se45 | 4.270 | 4.150 | DA47 |
| As-Se | As40Se60 | 4.590 | 4.661 | DA47 |
| As-S-Se | As32S34Se34 | 3.740 | 3.687 | DA47 |
| As-S-Se | As24S38Se38 | 3.630 | 3.538 | DA47 |
| As-S-Se | As18S41Se41 | 3.500 | 3.430 | DA47 |
| As-S | As24S76 | 2.670 | 2.667 | DA47 |
| As-S-Se | As24S57Se19 | 3.110 | 3.105 | DA47 |
| As-S-Se | As24S19Se57 | 4.050 | 3.915 | DA47 |
| As-Se | As24Se76 | 4.460 | 4.476 | DA47 |
| As-S-Se | As14S43Se43 | 3.430 | 3.361 | DA47 |

Note: Details for the glass compositions used in our study (see Figure 1)

References

[DA01]	Cui, S. (2014). Synthesis and characterization of tellurium based glasses for far infrared sensing and thermoelectric applications [Doctoral dissertation, Université Rennes 1]. TEL.

[DA02]	Pamukchieva, V., Szekeres, A., Todorova, K., Fabian, M., Svab, E., Revay, Zs., & Szentmiklosi, L. (2009). Evaluation of basic physical parameters of quaternary Ge–Sb-(S,te) chalcogenide glasses. Journal of Non-Crystalline Solids, 355(50-51), 2485-2490. https://doi.org/10.1016/j.jnoncrysol.2009.08.028

[DA03]	Borisova, Z. (2013). Glassy semiconductors. Springer.

[DA04]	Mel’nichenko, T. D., Fedelesh, V. I., Mel’nichenko, T. N., Sanditov, D. S., Badmaev, S. S., & Damdinov, D. G. (2009). On the approximate estimation of the surface tension of chalcogenide glass melts. Glass Physics and Chemistry, 35(1), 32-42. https://doi.org/10.1134/S1087659609010052

[DA05]	Musgraves, J. D., Wachtel, P., Novak, S., Wilkinson, J., & Richardson, K. (2011). Composition dependence of the viscosity and other physical properties in the arsenic selenide glass system. Journal of Applied Physics, 110(6), 063503. https://doi.org/10.1063/1.3638122

[DA06]	Shpotyuk, Ya., Bureau, B., Boussard-Pledel, C., Nazabal, V., Golovchak, R., Demchenko, P., & Polovynko, I. (2014). Effect of Ga incorporation in the As30Se50Te20 glass. Journal of Non-Crystalline Solids, 398-399, 19-25. https://doi.org/10.1016/j.jnoncrysol.2014.04.021

[DA07]	Olivier, M., Tchahame, J. C., Němec, P., Chauvet, M., Besse, V., Cassagne, C., ..., & Nazabal, V. (2014). Structure, nonlinear properties, and photosensitivity of (GeSe2)100-x(Sb2Se3)x glasses. Optical Materials Express, 4(3), 525-540. https://doi.org/10.1364/OME.4.000525

[DA08]	Dai, Y., Chen, S., Chen, C., & Wang, J. (1999). Glass formation, density, microhardness, and optical properties of As–Si–Te chalcogenide alloys. Journal of Non-Crystalline Solids, 255(2-3), 217-227. https://doi.org/10.1016/S0022-3093(99)00413-5

[DA09]	Amorphous Materials, Inc., (2024). Datasheets: AMTIR-glass series. https://www.amorphousmaterials.com/products/ .

[DA10]	Schott Glass Technologies, Inc., (2023). Datasheets: IRG-glass series. https://www.schott.com/en-us/products/infrared-glasses-and-materials-p1000261

[DA11]	Lonergan, J., Lonergan, C., McCloy, J., & Richardson, K. A. (2019). Modeling and experimental determination of physical properties of GexGaySe1-x-y chalcogenide glasses II: Optical and thermal properties. Journal of Non-Crystalline Solids, 511, 115-124. https://doi.org/10.1016/j.jnoncrysol.2019.01.034

[DA12]	Pethes, I., Nazabal, V., Chahal, R., Bureau, B., Kaban, I., Belin, S., & Jóvári, P. (2016). Local motifs in GeS2–Ga2S3 glasses. Journal of Alloys and Compounds, 673, 149-157. https://doi.org/10.1016/j.jallcom.2016.02.193

[DA13]	Loretz, T. J. (2020). Unpublished Laboratory Research Data made on Ge-As-Se-Bi Chalcogenide glass system melts, Computer Engineering Service.

[DA14] Petkova, T., Nedevaa, Y., & Petkova, P. (2001). Compositional trends of the properties in chalcogenide Ge-Se-Ga glasses.  Journal of Optoelectronics and Advanced Materials, 3(4), 855-860. https://old.joam.inoe.ro/arhiva/pdf3_4/Petkova.pdf.

[DA15]	Wang, X., Nie, Q., Wang, G., Sun, J., Song, B., Dai, S., ..., & Ma, H. (2012). Investigations of Ge–Te–AgI chalcogenide glass for far-infrared application. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 86, 586-589. https://doi.org/10.1016/j.saa.2011.11.018

[DA16]	Vassilev, V. (2006) Multicomponent Cd (Zn) containing Ge(As)-chalcogenide glasses. Journal of the University of Chemical Technology and Metallurgy, 41(3), 257-276.

[DA17]	Giridhar, A., Mahadevan, S., & Singh, A. K. (1984). Elastic properties of As-Sb-Se glasses. Bulletin of Materials Science, 6(6), 1001-1007. https://doi.org/10.1007/BF02743948

[DA18]	Kumar, R., Sharma, P., Sharma, P., & Rangra, V. S. (2011). Effect of Sn addition on physical properties of Se–Te glassy semiconductors. Journal of Non-Oxide Glasses, 3(2), 45–54.  https://www.researchgate.net/publication/228894269

[DA19]	Sharma, P., & Katyal, S. C. (2008). Effect of tellurium addition on the physical properties of germanium selenide glassy semiconductors. Physica B: Condensed Matter, 403(19-20), 3667-3671. https://doi.org/10.1016/j.physb.2008.06.009

[DA20]	Huddleston, J., Novak, J., Moreshead, W. V., Symmons, A., & Foote, E. (2015). Investigation of As₄₀Se₆₀ chalcogenide glass in precision glass molding for high-volume thermal imaging lenses. Infrared Technology and Applications XLI: Proceedings of SPIE, 9451, 94511O. https://doi.org/10.1117/12.2177026

[DA21]	Lopez, C. (2004). Evaluation of the photo-induced structural mechanisms in chalcogenide [Doctoral dissertation, University of Central Florida]. STARS. https://stars.library.ucf.edu/etd/207

[DA22]	Petkova, T., Ilcheva, V., Ilchev, P., & Petkov, P. (2013). Ge-chalcogenide glasses – properties and application as optical material. Key Engineering Materials, 538, 316-319. https://doi.org/10.4028/www.scientific.net/KEM.538.316

[DA23]	Crystran Ltd. (2021). Datasheet handbook. https://www.crystran.co.uk/handbook

[DA24]	Chahal, R., Starecki, F., Doualan, J.-L., Němec, P., Trapananti, A., Prestipino, C., ..., & Nazabal, V. (2018). Nd3+ : Ga-Ge-Sb-S glasses and fibers for luminescence in mid-IR: synthesis, structural characterization and rare earth spectroscopy. Optical Materials Express, 8(6), 1650. https://doi.org/10.1364/OME.8.001650

[DA25]	Saffarini, G. (1991). X-ray photoelectron spectroscopy (XPS), X-ray diffraction (XRD), differential scanning calorimetry (DSC) and density study of ternary chalcogenide glasses based on Ge-Se and Ge-S [Doctoral dissertation, Brunel University]. Brunel University Research Archive. https://bura.brunel.ac.uk/handle/2438/7396

[DA26]	Wang, T. (2017). Investigations on structure and properties of Ge-As-Se chalcogenide glasses [Doctoral dissertation, Australian National University]. ANU Open Research. https://openresearch-repository.anu.edu.au/server/api/core/bitstreams/cd2d5b7c-dbed-460c-bf57-9fa5359b9437/content

[DA27]	Sharda, S., Sharma, N., & Sharma, P. (2012). Basic physical analysis of new Sb-Se-Ge-In chalcogenide glassy alloys by predicting structural units: A theoretical approach. Chalcogenide Letters, 9(9), 389-395.

[DA28]	Kumar, K., Thakur, N., Katyal, S. C., & Sharma, P. (2010). A Study of the Physical Properties of Te15(Se100-xBix)85 Glassy Alloys. Defect and Diffusion Forum, 305-306, 61-69. https://doi.org/10.4028/www.scientific.net/DDF.305-306.61

[DA29]	Yang, G., Gueguen, Y., Sangleboeuf, J.-C., Rouxel, T., Boussard-Plédel, C., Troles, J., ..., & Bureau, B. (2013). Physical properties of the  GexSe1-x glasses in the 0<x<0.42 range in correlation with their structure. Journal of Non-Crystalline Solids, 377, 54-59. https://doi.org/10.1016/j.jnoncrysol.2013.01.049

[DA30]	Hu, J., Sun, X., Agarwal, A. M., Viens, J.-F., Kimerling, L. C., Petit, L., ..., & Richardson, M. (2007). Studies on structural, electrical, and optical properties of Cu doped As–Se–Te chalcogenide glasses. Journal of Applied Physics, 101(6), 063520. https://doi.org/10.1063/1.2712162

[DA31]	Hilton, R., Sr., Hayes, D. J., & Rechtin, M. D. (1974). Chalcogenide glasses for high energy laser application (Report No. AD-782 036). Office of Naval Research; Advanced Research Projects Agency. https://apps.dtic.mil/sti/html/tr/AD0782036/index.html

[DA32]	Anthonis, H. E. (1972). Polynary silicon tellurium glasses [Master’s thesis, University of Missouri–Rolla]. Scholars’ Mine. https://scholarsmine.mst.edu/masters_theses/3535

[DA33]	Richardson, K. (2018). Ge-As-Pb-Se (GAP-Se) chalcogenide glass systems [Unpublished laboratory data]. University of Central Florida.

[DA34] Guin, J.-P., Rouxel, T., Keryvin, V., Sanglebœuf, J.-C., Serre, I., & Lucas, J. (2002). Indentation creep of Ge–Se chalcogenide glasses below Tg: Elastic recovery and non-Newtonian flow. Journal of Non-Crystalline Solids, 298(2–3), 260–269. https://doi.org/10.1016/S0022-3093(01)01053-5

[DA35]	Li, J., Xia, K., Gu, J., Zheng, W., Zhang, J., Liu, Y., ..., & Liu, Z. (2023). Refractive index improvement of commercial chalcogenide glasses by external doping with Ag and Pb. Optical Materials Express, 13(6), 1700-1709. https://doi.org/10.1364/OME.489361

[DA36]	Yuan, B. (2022). Structural control on the viscoelastic behavior and shear relaxation in chalcogenide glass-forming liquids [Doctoral dissertation, University of California, Davis]. eScholarship. https://escholarship.org/uc/item/6kt7h318

[DA37]	Hristova-Vasileva, T., Aljihmani, L., & Vassilev, V. (2014). Physical properties of chalcogenide glasses from the GeSe₂-Sb₂Te₃-PbSb₂Te₄ system. Materials Science: An Indian Journal, 10(10), 410–415.

[DA38]	Wavelength Opto-Electronic (S) Pte Ltd. (n.d.). Sulphur based chalcogenide glass [Datasheet]. https://wavelength-oe.com/wp-content/uploads/Chalcogenide-Materials.pdf

[DA39]	Liu, K., Kang, Y., Tao, H., Zhang, X., & Xu, Y. (2022). Effect of Se on structure and electrical properties of Ge-As-Te glass. Materials, 15(5), 1797. https://doi.org/10.3390/ma15051797

[DA40]	Hubert, M. (2012). Chalcogenide glasses for infrared applications: New synthesis routes and rare earth doping [Doctoral dissertation, University of Arizona]. ProQuest Dissertations & Theses.

[DA41]	Carlie, N. (2010). A solution-based approach to the fabrication of novel chalcogenide glass materials and structures [Doctoral dissertation, Clemson University]. Clemson University. https://open.clemson.edu/all_dissertations/554

[DA42].	Sharma, R., Marro, J., Howe, A., Kosan, C., Kocher, M., Whetstone, J., ..., & Richardson, K. A. (2025). Investigation of optical and mechanical properties of sulfur doped GeSe2-Ga2Se3–CsCl multispectral glass. Optical Materials, 168, 117409. https://doi.org/10.1016/j.optmat.2025.117409

[DA43]	Masselin, P., Coq, D., Calvez, L., Petracovschi, E., Lépine, E., Bychkov, E., & Zhang, X. (2012). CsCl effect on the optical properties of the 80GeS2–20Ga2S3 base glass. Applied Physics A, 106(3), 697-702. https://doi.org/10.1007/s00339-011-6668-6

[DA44]	Ledemi, Y., El-Amraoui, M., Calvez, L., Zhang, X.-H., Bureau, B., & Messaddeq, Y. (2013). Colorless chalco-halide Ga₂S₃-GeS₂-CsCl glasses as new optical material. Proceedings of SPIE, 8847, 884704. https://doi.org/10.1117/12.2024461

[DA45]	Kebaili, I. (2021). The effect of adding CsCl content on physicochemical properties of (Ges2–sb2s3)100-x(Cscl)x (0 ≤ x ≤ 40 mol%) chalcogenide glass ceramics. Optical Materials, 119, 111363. https://doi.org/10.1016/j.optmat.2021.111363

[DA46]	Carcreff, J., Masselin, P., Boussard-Plédel, C., Kulinski, P., Troles, J., & Coq, D. L. (2020). Step-index fibre from metal halide chalcogenide glasses. Optical Materials Express, 10(11), 2800-2812. https://doi.org/10.1364/OME.408334

- [DA47] Richardson, K., Cardinal, T., Richardson, M., Schulte, A., & Seal, S. (2003). Engineering glassy chalcogenide materials for integrated optics applications. In A. V. Kolobov (Ed.), Photo-induced metastability in amorphous semiconductors (pp. 383-406). Wiley-VCH. https://doi.org/10.1002/9783527602544.ch23